|  | ECO-Shell Walnut Shell Media For Water Filtration, Abrasive Blasting and Industrial Applications |  |
| --- | --- | --- |

| Technical Specifications |
| --- |
| Physical Properties | Shipping Information |
| Color | Light Brown | Weight per Bag | 50 LBS |
| Modulus of Elasticity | 22,900 PSI | Bags per Pallet | 40 - 50# Bags |
| Specific Gravity | 1.2 | Pallet Size | 40” X 48” |
| Displacement | 0.375” @ 5,400 PSI | Weight per Pallet | 2,000 LBS |
| Solubility | Not soluble in water | Methods of Shipment | Flatbed, Rail and Overseas Container |
| Mesh Sizes Available | 4-6; 4-20; 6-10; 8-12; 12-20; 14-30; 18-40; 20-30; 20-40; 40-60; 40-100; 100; 200 | Supply Availability | 400 Metric Tons per Week |
| Applications | Produced water, filter media, abrasive blasting, cosmetics, filler or extender |

# Text boxes

Eco-Shell walnut shell media is a by-product of English walnut shell trees from the Sacramento Valley in California. The various mesh sizes are milled and processed at a state of the art facility in Corning, CA.

The processed walnut shells are used for various industrial applications such as removal of free oil from produced water, abrasive blasting, cosmetic exfoliates, fillers, and production of activated carbon.

The walnut shell media is competitively priced and available from stock.

For information on how to order ECO-Shell walnut shell media, please contact K2O Consulting.

Picture of Walnut Shell Media