|  | ECO-BURNTM Bio-Fuel For High BTU Low Cost Renewable Fuel |  |
| --- | --- | --- |

| Technical Specifications |
| --- |
| Physical Properties | Shipping Information |
| Color | Brown to Black | Weight per Bag | 40 LBS |
| BTU Rating | 8,900 – 9,200 BTU’s | Bags per Pallet | 40 |
| Ash Content | 1.0 – 1.5% | Pallet Size | 40” X 48” |
| Formulation | Agricultural By-Products | Weight per Pallet | 2,000 LBS |
| Bulk Density | 40 LBS / ft3 | Methods of Shipment | 44 Ton Rail Car or Container |
| Moisture | 6 – 8% | Supply Availability | 400 Metric Tons per Week |
| Applications | Multi-Fuel Furnaces, Boilers and Stoves |

# Text boxes

Eco-BURNTM pellet fuel is produced from agricultural by-products. The raw materials are annually renewable which provides a consistent supply year after year. No binding agents are used which ensures an all natural fuel. ECO-BURNTM burns hotter than corn and most wood pellets. This translates to substantial savings in fuel costs.

ECO-BURNTM is currently being used in Multi-Fuel Stoves, Boilers, Furnace Systems, small scale Co-Generation Plants and Stoker Systems. It can be shipped by rail or by common carrier. Choosing ECO-BURNTM for your fuel source means that you have chosen to burn “GREEN”.

For information on how to order ECO-BURNTM, please contact K2O Consulting.